## Slide 1
ICMNE-2023
Study of SiO2 based MOS by capacitance-voltage and thermally stimulated current techniques
R. Aliasgari Renani*, O.A. Soltanovich, M.A. Knyazev,
and S.V. Koveshnikov
Institute of Microelectronics Technology, RAS, Chernogolovka, Russia
* MIPT, Dolgoprudny, Russia
10/4/2023

## Slide 2
SiO2 applications, requirements and issues Applications:
Major gate dielectric for Si, SiC, GaN MOSFETs
Passivation layer for bipolar transistor IC, Flash Memory, etc.
Active layer for resistive memory
etc.
Requirements:
Stability under bias stress
Radiation immunity under high and low energy irradiation
Low density of bulk traps and states at the interface with semiconductor
etc.
Issues:
Bulk traps for electrons and holes and interface states as revealed by C-V method
Quality of thin (less than 10 nm) oxide
Needs for good metrology
ICMNE-2023
10/4/2023

## Slide 3
Defect generation in SiO2: Motivation and Objective
Low energy e-beam irradiation:
Generation of positive charge mainly
at the SiO2/Si interface revealed by C-V
High-energy gamma-irradiation:
Generation of interface states
Hydrogen passivation in ECR plasma:
Etching of SiO2 and generation of
positive charge
Objective: investigate properties of defects generated in MOS by using both methods:
capacitance –voltage and thermally stimulated current
ICMNE-2023
10/4/2023

## Slide 4
4
Method of Thermally Stimulated Current (TSC)
ICMNE-2023
Cooling down under reverse bias → traps not filled with carriers
(2) Charge injection/ Filling: → traps filled by applying bias or via optical injection
(3) Measurement: temperature is raised with a constant rate under reverse bias
(4) Recording TSC-spectra: → monitoring the discharging current due to thermal emission from the defect levels

## Slide 5
Reverse bias
during cooling
Forward bias
at LT w/o
e injection
Forward bias
at LT with
e injection
Method of Thermally Stimulated Current:
Choosing measurement conditions based on C-V data
Reverse bias
during measurement
Ec
EF
EV
e
Ec
EF
EV
Ec
EF
EV
+
Ec
EF
EV
ICMNE-2023
10/4/2023

## Slide 6
Method of Thermally Stimulated Current:
Everbeing Cryo station (80K – 450K)
with 4 micromanipulators and Lake Shore
Temperature controller
TSC experimental setup with originally
developed software
Parametric Analyzer Keithley 4200A-SCS
Source Meter Keithley 2450
Keysight 2987 Electrometer (sensitivity 10 fA)
ICMNE-2023
6
10/4/2023

## Slide 7
e-beam irradiated n-MOS: C-V
n-MOS structures irradiated in Jeol JSM 840A with 20 keV electrons, dose 500 mC
Notable changes observed after e-beam irradiation:
  shift to negative voltage is due to positive charge in SiO2 bulk
  decreased C-V slope is caused by increased density of interface states
  hysteresis indicates formation of “shallow” electron traps in the oxide bulk
  increasing negative bias reveals deep and shallow traps for holes in the oxide
C-V slope indicates uniform increase of Dit over the band gap - is it so?
How shallow are the “shallow” traps? (up to ~0.7 eV traps emit electrons at RT)
start
start
ICMNE-2023
10/4/2023

## Slide 8
e-beam irradiated n-MOS: TSC
E3
Ec
EF
EV
Ec
EF
EV
During pulse
Ec
EF
EV
During warming
E2
E1
During pulse
Different portions of BG for interface states +
same shallow electron traps contribute to TSC
During pulse
E1
E2
E3
E4
E5
Ec
EF
EV
Ec
EF
EV
Ec
EF
EV
+
During warming
During warming
Preliminary trap identification:
E1 – electron traps in Si within the space charge region; E2 – int. states
Lower pulse eliminates electron
injection and trapping
Same cooling and pulse
Same bias during warming
E6
ICMNE-2023
10/4/2023

## Slide 9
e-beam irradiated n-MOS: TSC
To identify traps, the measurements done
under conditions eliminating contribution of interface states and electron traps
E1
E2
E3
E4
E5
E7
E3
During pulse
During measurement
Ec
EF
EV
+
+
h
Ec
EF
EV
Thus, E3 and E7 are related to shallow hole traps in SiO2
ICMNE-2023
10/5/2023
Onle hole traps contribute to TSC

## Slide 10
E6 is a shallow electron trap as it is seen only at low E field;
At high E field the electrons are blown out from shallow traps and not detected
Identification of traps in TSC spectrum
ICMNE-2023
10/5/2023
Pulse | Bias at Warming | Peaks in TCS spectra | Identification
+10V (accumulation, electron injection) | -5.5V (strong depletion; hole injection; int. states all over contribute to TSC) | E1, E2, E3 | E1 – electron traps in Si; E2 – int. states; E3 - hole traps in SiO2
+1V (accumulation, no electron injection) | -5.5V (strong depletion; hole injection; all int. states contribute to TSC) | E2, E3, E6 | E2 – int. states; E3 - hole traps in SiO2 E6 - electron trap in SiO2
-10V (strong depletion, hole injection) | +1V (accumulation; int. states are filled and do not contribute to TSC) | E3, E7 | E3 - hole traps in SiO2 E7 - hole traps in SiO2
+10V (accumulation, electron injection) | -2.5V (weak depletion; only a portion of BG int. states contributes to TSC) | E4, E5 | E4, E5 – int. states and/or electron traps in SiO2
Identification of traps is done based on knowledge of the part of MOS structure to be
tested and what carriers were injected and trapped

## Slide 11
TSC spectra of gamma irradiated and hydrogen plasma treated MOS structures
ICMNE-2023
10/5/2023
Gamma irradiation
Hydrogen plasma treatment
Radiation defects in Si
Electron traps in ultra thin SiO2

## Slide 12
Summary
We have investigated traps generated in Si/SiO2 structures by low energy electron irradiation, high energy gamma rays and hydrogen plasma
Based on the obtained data and gained experience we can conclude:
TSC is a highly sensitive method to detect traps in MOS devices
TSC can be applied to investigation of any dielectric/semiconductor structure and semi-insulating materials (e.g., GaAs)
With help of C-V, traps revealed by TSC can be identified :
  by their location (within dielectric, semiconductor or at the interface)
  by their nature (trap for electron or for hole)
Utilization of highly sensitive electrometer (e.g., Keysight B2987A) for current measurements will allow evaluation of trap activation energy
ICMNE-2023
10/4/2023

## Slide 13
Current meters for TSC
ICMNE-2023
10/4/2023

## Slide 14
Back Up